## Slide 1: Morphology and EDX mapping of Mg1-xNixO
S36328 – 2.5%Ni in MgO
Gregor Koch 3rd February 2023

## Slide 2
Morphology is invariant compared to analogous samples
Disc-like morphology with narrow disc size distribution
High magnification not clearly indicated small pores in this sample but it is not excluded or must be confirmed in an additional measurement
No indications for any segregated NiO phases (neither EDX nor SEM)
No impurities according to EDX and homogeneous composition
Suggested formulas:
S36328: Ni0.037±0.002Mg1±0.043O1.24±0.042
S34869: Ni0.01±0.0004Mg1.00±0.08O1.49±0.07
S35123: Ni0.106±0.004Mg1.00±0.08O2.15±0.06
S35146: Ni0.23±0.01Mg1.00±0.13O1.83±0.07
Errors due to shadowing in each map (overestimation in perfectly distributed Ni in MgO) can be likely. Variation of results of all maps is given in the little grey table
S36328 in comparison to S34869, S35123, S35146
Mg1-xNixO
at% | Map1 | Map2 | map3 | Map4 | mean | sd | rsd / %
Mg/Ni | 26.40 | 29.63 | 23.99 | 27.66 | 26.92 | 2.36 | 8.78
Mg/O | 0.82 | 0.87 | 0.73 | 0.82 | 0.81 | 0.06 | 7.53
Ni/O | 0.03 | 0.03 | 0.03 | 0.03 | 0.03 | 0.00 | 2.30
Ni/(Mg+Ni) | 0.04 | 0.033 | 0.04 | 0.03 | 0.04 | 0.00 | 8.61

## Slide 3
S36328

## Slide 4
S36328
Exactly the same impression like I had in the previous measurements of the other samples

## Slide 5
S36328
Can be little pores, however I could not improve the settings for better resolution

## Slide 6
S36328 – map1
Element | Mass [%] | Mass Norm. [%] | Atom [%] | abs. error [%] (1 sigma) | rel. error [%] (1 sigma)
Oxygen | 43.1 | 42.5 | 54.1 | 1.8 | 4.1
Magnesium | 53.5 | 52.7 | 44.2 | 2.1 | 4.0
Nickel | 4.9 | 4.8 | 1.7 | 0.1 | 2.7
 | 101.6 | 100.0 | 100.0 |  | 

## Slide 7
S36328 – map1

## Slide 8
S36328 – map2
Element | Mass [%] | Mass Norm. [%] | Atom [%] | abs. error [%] (1 sigma) | rel. error [%] (1 sigma)
Oxygen | 43.9 | 41.1 | 52.6 | 1.8 | 4.1
Magnesium | 58.1 | 54.4 | 45.8 | 2.3 | 3.9
Nickel | 4.7 | 4.4 | 1.5 | 0.1 | 2.5
 | 106.8 | 100.0 | 100.0 |  | 

## Slide 9
S36328 – map2

## Slide 10
S36328 – map3
Element | Mass [%] | Mass Norm. [%] | Atom [%] | abs. error [%] (1 sigma) | rel. error [%] (1 sigma)
Oxygen | 44.2 | 45.2 | 57.0 | 1.8 | 4.1
Magnesium | 48.7 | 49.8 | 41.3 | 1.9 | 3.9
Nickel | 4.9 | 5.0 | 1.7 | 0.1 | 2.6
 | 97.8 | 100.0 | 100.0 |  | 

## Slide 11
S36328 – map3
cubes

## Slide 12
S36328 – map4
Element | Mass [%] | Mass Norm. [%] | Atom [%] | abs. error [%] (1 sigma) | rel. error [%] (1 sigma)
Oxygen | 43.0 | 42.5 | 54.1 | 1.8 | 4.1
Magnesium | 53.4 | 52.8 | 44.3 | 2.1 | 3.9
Nickel | 4.7 | 4.6 | 1.6 | 0.1 | 2.4
 | 101.0 | 100.0 | 100.0 |  | 

## Slide 13
S36328 – map4